Here is a complete setup package tailored for Fired Arts Studio, including a studio safety Standard Operating Procedure (SOP), an event production batch schedule, and an interactive tool to model material costs and event margins.

## 1. Studio SOP: Mold Making & Slip Casting (Contamination-Safe)

Because raw plaster particles ruin fired pottery by absorbing moisture, expanding, and causing surface pop-outs during glaze firings, strict separation protocols are essential.

## Zone Setup & Prep

- Dedicated "Plaster Zone": Confine all dry plaster mixing, sanding, and de-molding to the utility/back-of-house wash sink area. Never mix or sand plaster in customer paint areas or near raw glaze containers.

- PPE & Safety: Wear an N95 dust mask and eye protection when scooping and sifting dry Pottery Plaster #1.

- Sink Discipline: Never wash wet plaster down studio drains. Use a three-bucket settling system to let plaster solids precipitate out, disposing of the hardened pucks in solid trash.

## Pouring & Casting Protocol

- Model Release: Ensure the 3D-printed master from your Flashforge AD5X is sealed with acrylic gloss and coated with Murphy’s Oil Soap.

- Plaster Mixing (100:70 Ratio): Slowly sift 70 parts water to 100 parts plaster by weight across the surface. Let slake for 2 minutes, then gently hand-mix to eliminate air bubbles before pouring around the master.

- Mold Curing: Allow fresh plaster to cure for 45–60 minutes before opening. Let the mold dry in a warm area (or near kiln ambient heat, below 120°F) for 3–5 days until fully dry.

- Slip Casting Run: Pour low-fire casting slip (Cone 04–06) into the mold until full. Top off as the plaster absorbs water. After 15–20 minutes (for an 1/8" to 3/16" wall), pour excess slip back into the storage bucket.

- Fettling & Firing: Once leather-hard (2–4 hours), demold. Trim the pouring sprue and use a damp sponge to smooth seam lines. Dry to bone-dry, then load into your regular weekly bisque cycle.

## 2. Event Batch Scaling Schedule (Target: 25 Custom Pieces)

To run a special VIP Workshop (such as a custom Kokomo landmark planter or local mascot night) without disrupting daily studio floor operations:

- Molds Needed: 4 to 5 working plaster molds (cast in-house from 1 or 2 3D prints).

- Lead Time: 2 Weeks prior to the workshop date.

| Day / Timeline | Phase | Daily Task |
| --- | --- | --- |
| Week 1: Mon–Tue | 3D Printing | Run 1–2 master models on the Flashforge AD5X (layer height 0.12mm, filler primer + sand). |
| Week 1: Wed–Thu | Tooling | Cast 4–5 plaster working molds in the back utility area. |
| Week 1: Fri–Sun | Mold Curing | Allow plaster molds to dry completely near kiln exhaust. |
| Week 2: Mon | Casting Run 1 | Cast 2 batches across 4 molds (8 pieces poured & demolded). |
| Week 2: Tue | Casting Run 2 | Cast 2 batches across 4 molds (8 pieces poured & demolded). |
| Week 2: Wed | Casting Run 3 | Cast 2–3 batches across 4 molds (9–10 pieces to reach 25–26 total units). |
| Week 2: Thu–Fri | Drying | Bone-dry greenware on back racks; sponge and fettle rims. |
| Week 2: Sat | Bisque Fire | Load all 25 pieces into the weekly Cone 04 bisque kiln alongside regular studio stock. |
| Week 2: Sun | Shelf Staging | Unload, inspect, label, and stage on the event tables ready for customer glaze painting. |

If you'd like to adjust this for an upcoming studio project, I can:

- Provide OpenSCAD parameters for a specific custom shape or local icon.

- Help select a low-fire casting slip brand compatible with the studio's current Mayco glazes.