The Flashforge Adventurer 5X (AD5X) is a high-speed FDM (Fused Deposition Modeling) plastic printer. Because it prints in plastic (PLA, PETG, ABS), you cannot print functional clay items directly. Instead, your workflow will focus on Method 1: Printing a plastic Master Model to cast a plaster slip-casting mold.

Here is your step-by-step post-processing and preparation guide for using the Flashforge AD5X to create PYOP blanks.

## 1. Slicer and Print Settings (FlashPrint / OrcaSlicer)

To get a smooth master model that releases cleanly from plaster, use these optimized settings:

- Layer Height: 0.12mm to 0.16mm (Standard 0.4mm nozzle). Thinner layers mean less sanding later.

- Wall Loops: 3 to 4 perimeters. You will be sanding the model heavily; extra walls prevent you from sanding through to the hollow infill.

- Infill: 15% to 20% Gyroid. Provides structural strength against the weight of wet plaster.

- Material: PLA is cheapest and easiest to sand. PETG is also excellent if you need higher chemical resistance against mold release agents.

## 2. Eliminating 3D Print Lines (Critical Step)

Plaster captures microscopic details. If you leave raw 3D print layer lines on your plastic master, the plaster mold will lock onto those ridges, tearing your clay pieces when you try to demold them.

- Coarse Sanding: Use 120-grit wet/dry sandpaper to knock down the worst of the 3D print layer ridges.

- Filler Primer: Spray the model with 2–3 coats of automotive filler primer. This heavy spray settles into the micro-gaps between layers.

- Fine Sanding: Once dry, sand the primer using 320-grit, then 400-grit sandpaper until it feels as smooth as glass.

- Sealing: Spray a final coat of clear gloss acrylic sealer. A glossy surface releases flawlessly from wet plaster.

## 3. Setting Up the Plaster Pour

- The Cotter Box: Build a rigid box around your scaled-up plastic master using acrylic sheets, LEGO blocks, or scrap wood.

- Secure the Base: Hot glue your plastic model to the bottom of the box so it doesn't float when the heavy liquid plaster is poured in.

- Release Agent: Thoroughly coat the plastic master and the inside of the box with Potter’s Soap (Murphy’s Oil Soap) or a dedicated mold release spray. Wipe away any pooling.

- Pouring Plaster: Mix Pottery Plaster #1 (standard for slip casting because of its water absorption rates). Pour it slowly into a corner of the box, letting it rise up around the model to prevent air bubbles from getting trapped on the details.

## 4. Flashforge AD5X Considerations

- Bed Adhesion: The AD5X has a textured PEI plate. The bottom of your master model will inherit this texture. Ensure the textured face is either the sacrificial bottom of the piece (where the pour spout will go) or sand it completely flat.

- Enclosure Advantage: If your master model has sharp, 90-degree corners, print with the AD5X top cover/door closed (if using PETG or ABS) to prevent the corners of your master model from warping off the bed.

If you want to start designing, tell me:

- Are you designing a 1-piece open mold (like a flat plate or simple bowl) or a multi-part mold (like a 2-piece hollow mug or figurine)?

- What software (e.g., Blender, Fusion 360, Tinkercad) do you plan to use?

I can walk you through how to digitally slice your model into a multi-part mold assembly.